## Slide 1: WFIRST Coronagraph Detector Requirements
These are the noise and efficiency requirements for the WFIRST coronagraph detector. Functionality requirements also apply. The coronagraph Science investigation teams will be defining the threshold science case. We expect that the capability-based requirements below will meet the threshold science.
The basis of these requirements is the already-achieved end of life EMCCD performance, as well as a detection and characterization SNR model.
The following conditions must be applied when evaluating detectors against these requirements:
  Detector is at the end of life for the WFIRST mission (6 years at L2)
  Incident flux from all photon sources is e-/pixel/frame
  Detection is in the photon counting mode
  The detector is no colder than -105o C or 168 K
Conversion Efficiency
  Defined as the fraction of times a single incident photon is counted as a single photon and includes
    Quantum Efficiency
    Charge transfer efficiency (where applicable)
    Photon counting efficiency (thresholding efficiency)
Total Noise from one pixel in a 100-second frame
  Defined as the standard deviation of the combined detector noise contributions from:
    Read noise
    Dark current
    Clock induced charge (CIC, where applicable)
Conversion efficiency | Imaging 1 | Imaging 2 | IFS 1 | IFS 2
 | 450 nm | 565 nm | 660 nm | 770 nm
 | 10% | 10% | 18% | 18%
@ | 23% | 24% | 23% | 18%
Conversion efficiency | Imaging 1 | Imaging 2 | IFS 1 | IFS 2
 | 450 nm | 565 nm | 660 nm | 770 nm
 | 10% | 10% | 18% | 18%
 | 23% | 24% | 23% | 18%
Combined Noise | 1 pixel, 100s frame, at
 | 0.27 e-
Combined Noise | 
 | 0.27 e-

## Slide 2: Backup information for CGI system engineering
Conversion efficiency
  Three sources were considered
    E2v QE for basic Multi2 std Si
    Measured charge transfer loss in lab
    Modeled threshold efficiency for photon counting
Total Noise
  Started with the phase II irradiated EMCCD representing EOL conditions:
    read noise (assume 50e- and gain of 1000),
    dark current as measured in lab, and
    CIC as measured in lab.
  Computed the sqrt of sum of variances
    is a variance
    is effectively a variance
    is an effective read noise and is a standard deviation
a
b
c